STUC-O-FLEX

DIRECT APPLICATION TO METAL

MANUFACTURERS SPECIFICATION / SECTION 09960

PART 1-GENERAL

1.00 SCOPE

Manufacturer's specifications containing the requirements necessary for proper installation of the STUC-O-FLEX finish coating over properly prepared Metal substrates.

1.01 DESCRIPTION

A. Provide all labor, materials, and equipment  necessary to install the field 	applied STUC-O-FLEX finish coating.

B. Related work specifications (as required):

1. Sealant 07900

1.02 QUALITY ASSURANCE

- Testing - Finish shall meet standards as outlined below:

| TEST | METHOD | RESULT |
| --- | --- | --- |
| ELONGATION % (FINISH) |  | 105 Percent |
| WATER VAPOR TRANSMISSION | ASTM-E96 | 14 GRAINS PER HOUR / SQ. FT. (AVERAGE) |
| SALT SPRAY RESISTANCE | B-117 | 300 HOURS NO DELETERIOUS EFFECTS |
| ACCELERATED WEATHERING | G-23-81 | 2000 HOURS NO DELETERIOUS EFFECTS |
| ABSORPTION FREEZE THAW | 60 CYCLES | NO CRACKING, CHECKING |
| TENSILE BOND STRENGTH | ASTM C-297 | 95.9 PSI INCLUDES PRIMER |
| WATER PENETRATION TEST | ASTM-E-331 | NO WATER PENETRATION OCCURRED ON SUBSTRATE |
| WATER RESISTANCE TEST | ASTM D-2247 | NO CRACKING, BLISTERING, PEELING OR COMPROMISE |
| MILDEW / FUNGUS RESISTANCE | 810 B | NO MOLD OR MILDEW GROWTH DURING TEST |
| WIND DRIVEN RAIN |  | NO DELAMINATION NO WATER INTRUSION |
| FIRE TESTING TUNNEL TEST | ASTM E-84 | FLAME SPREAD < 25 SMOKE DEVELOPED < 450 CLASS "A" FIRE RATED |

NOTE: ADDITOINAL TEST RESULTS AND DATA AVAILABLE UPON REQUEST

1. Finish shall contain only Calcium Aggregates absent Silica Sand

2. Finish shall be comprised of only 100% Acrylic Polymer binders

3. Finish shall exceed 105% elongation

4. Finish shall have in excess of 250 million square feet in-service.

5. Finish shall exceed a 1/16” mandrel bend test without rupture of the 			membrane

6. Finish shall be manufactured in the United States of America

Technical Support Contact 1-800-305-1045 or e-mail 		technicalservice@stucoflex.com

1.03 GENERAL

A. The minimum slope of any surface shall not be less than 6" in 12".

B. To insure long-term performance, the system shall be engineered with regard 	for intended installation.

C. Expansion joint details required as specified by the design professional in 	addition to; where dissimilar materials abut, in conjunction with building 	expansion joints and where extreme structural movement may occur.

D. All surfaces shall be clean, dry, and free dust, dirt, mildew, form oils, grease, 	laitance and foreign materials.

E. Any and all loose, flaking, or oxidized materials on the surface shall be 	thoroughly addressed by sand blasting, pressure washing, sanding, and/or wire 	brush prior to Panel Prime, other Primers or Stuc-O-Flex Finish.

F. Caulking details, flashings, and terminations shall insure no water intrusion 	behind Stuc-O-Flex finish or substrate.

G. Some maintenance may be required to assure continued performance of 	properly detailed terminations.

1.04 SUBMITTALS

A. Samples:

1. The applicator shall, before the project commences, provide the owner 		or architect, a sample of suitable size of each color and texture as 				specified for the project for purposes of obtaining approvals.

2. Each sample shall be prepared using the same tools and techniques as 			required for the actual application.

3. An approved sample shall be available and maintained at the job site.

1.05 PRODUCT DELIVERY, STORAGE AND HANDLING

A. Deliver all material supplied by the manufacturer in original, unopened 	packages with legible manufacturer’s identification and labels intact.

B. Store all products supplied by STUC-O-FLEX in a cool dry place, out of direct 	sunlight, protected from weather and other damage. In addition, the materials 	shall be stored in tightly sealed containers at a temperature of not less than 40ºF 	at all times.

1.06 JOB CONDITIONS

A. Ambient temperatures shall be 40(F or greater at time of installation, and will 	remain so for a minimum 24 hours or protection and heat must be supplemented 	to insure proper drying.

- Product installation shall not take place during inclement weather unless 	adequate protection is provided both during application and until cured.  	Protect materials from rain until dried.

C. High humidity conditions (fog, mist, etc.) will significantly extend drying time

1.07 COORDINATION AND SCHEDULING

A. The work in this section requires close coordination with related sections and 		trades.

B. The tops of all walls must immediately be protected to prevent water infiltration 	behind the exterior wall assembly. The cap flashing should be installed 	immediately after the Finish coat has been cured.

C. Sealant and waterproofing materials shall be installed in a timely manner as to 		prevent water intrusion behind the Stuc-O-Flex coatings.

1.08  MAINTENANCE

A. Sealant and other components of the building must be inspected periodically 	to confirm performance as originally installed. Corrections shall be made at 	once.

1.09  LIMITED WARRANTY

Upon  proper installation of Stuc-O-Flex Finish a Standard Product Warranty will be issued.

Contact Stuc-O-Flex International, Inc. for on Warranty information @ 1-800-305-1045.

PART 2 - PRODUCTS

2.01  GENERAL

A. In  accordance with these specifications all products required for the

installation shall be obtained from STUC-O-FLEX INTERNATIONAL unless otherwise 	approved in writing. Contact:

Stuc-O-Flex International, Inc.		1-800-305-1045

17639 NE 67th Court			info@stucoflex.com

Redmond, WA 98052			www.stucoflex.com

2.02  MATERIALS

A. PRIMER,  Pre-primed metal surfaces will not require additional primers in most 	cases. Kynar, Polyester or Urethane coatings may require primer application prior 	to Stuc-O-Flex Finish application / Adhesion tests should be conducted.

(Contact Technical Center @ 1-800-305-1045)

B. STUC-O-FLEX FINISH, finish coat as manufactured by STUC-O-FLEX 	INTERNATIONAL, INC. is a factory premixed, 100% acrylic based, thermo plastic, 	color integrated, textured finish for use with this application. Numerous textures 	can be achieved using a variety of application methods. Spray applied or hawk 	& trowel - Sand finish, skip trowel, knock down, lace, etc. Provided in 20 standard 	colors, special colors upon request, See STUC-O-FLEX standard color chart.

C. WATER, shall be clean and potable in clean containers without any residue or 	foreign materials.

D. SEALANT (CAULKING), Shall be of appropriate quality to prevent potential 	water intrusion. Consult manufacturers for specific details and specification.

2.03  MIXING AND PREPARATION

A. PRIMER: Mix to manufacturers recommendations.

B. STUC-O-FLEX finish coat: Using a jiffler paddle type mixer agitate material until a 	homogeneous consistency is obtained. Care should be taken so as NOT to 	introduce air into finish coat material.

- Never add modifiers, admixtures or other products not specified to any

STUC-O-FLEX manufactured products.

PART 3 – EXECUTION

3.01 INSPECTION

A.  Substrate shall be examined for compliance with construction documents and 	system specifications prior to installation Stuc-O-Flex Finish.

B. Architect and General Contractor will be made aware of any such substrate 	concerns.  All problem areas shall be rectified before installation may continue.

C. Details for proper sealant joints shall be required.

D. Substrates and Primers will have been addressed as set forth in these 	specifications.

3.02 INSTALLATION

A. PRIMER (As required):  Apply primer with airless sprayer, medium nap roller, or 	paint brush as recommended by manufacturer to all areas where Stuc-O-Flex 	finish coat is to be applied. A uniform pinhole free layer should be provided to 	insure complete coverage of wall surface. Allow to dry completely.

B. STUC-O-FLEX ACRYLIC FINISH COAT, Apply in color and texture as approved by 	Architect and/or Client using stainless steel trowels or appropriate spray 	equipment with sufficient manpower and equipment to insure a continuous 	operation without cold joints, scaffolding lines, etc. Finished wall sections shall 	match approved job site sample. Coverage and thickness shall vary depending 	on texture desired and specified final appearance.

C. Mix STUC-O-FLEX prior to use with paddle type blade to insure consistency.

Small amounts of water may be added to adjust viscosity, 16oz. maximum per 5-	gallon pail.

D. Apply Stuc-O-Flex finish coat as to completely cover all areas of the metal 	surface with a nominal 1/16” thickness.

3.03 JOB SITE CLEAN UP

A.  STUC-O-FLEX applicator shall remove all excess wall system materials from 	completed project areas.

B.  Coverings, scaffolds, etc. shall be removed.