- STUC-O-FLEX

- THERMAL-FLEX

- COATING ASSEMBLY TO INSULATION BOARD

MANUFACTURERS SPECIFICATIONS / SECTION 07240

- PART 1 - GENERAL

- 1.01	DESCRIPTION

Provide all labor, materials and equipment necessary to install the “THERMAL-FLEX” Coating Assembly from STUC-O-FLEX. The assembly consists of PRM or Stuc-O-Base, a polymer modified cement adhesive / base coat, reinforcing fiberglass mesh, and Stuc-O-Flex finish applied to insulation board.

B.	Related work specified elsewhere:

1.	Sealant section 07900.

C.	Terms and Definitions:

1.	Thermal-Flex Assembly

Consists of STUC-O-FLEX reinforcing fiberglass mesh, adhesive / base coat, and 			finish coat, applied to insulation board.

2. 	PRM or Stuc-O-Base Adhesive / Base Coat

Cementitious, co-polymer base and adhesive, field mixed for use as an 				adhesive for approved insulation and base coat for reinforcing fiberglass mesh.		3.	Insulation Board

Expanded Polystyrene (EPS) Board with an average density of 1.0 pcf, a flame 			spread rating of less than 25, a smoke development index of less than 450 and 			an R-value of 3.85 per inch at 75 degrees F.  It must conform to ASTM C 578-85 			Class A.

Option:

Fiberglass faced Polyisocyanurate Insulation Board with an average density of 2.0 pcf, 		a flame spread rating of less than 25, a smoke development index of less than 450 			and an R-value of 3.85 per inch at 75 degrees F.  It must conform to ASTM C 578-85 			Class A

4.	Washers / Mechanical Fasteners

(optional / as required over secondary moisture barrier).

Shall be a 2” inch wide polypropylene washer with a recessed center chamber 			to accept the corrosion resistant fastener as manufactured by Wind-Lock or 				equal.

5.	Reinforcing Fiberglass Mesh

Balanced open weave reinforcing fiberglass mesh treated for compatibility with 			base coat materials.  The fabric shall not be less than 4.4 oz (± 10%) per square 			yard.

High Impact Resistant (Recommended for first floors, for high traffic areas, and areas subject 	to abuse). This consists of an additional layer of Light Armor (15 oz.) Mesh or Armor (21 oz.) 	mesh embedded into STUC-O-FLEX PRM or Stuc-O-Base base.  The heavier mesh is always 	installed under the lighter mesh.  In no case should Armor mesh be used without the regular 	mesh (4.4 oz) over it.

6.	Base coat

PRM (Polymer Reinforced Mortar) Base or Stuc-O-Base is a fiber reinforced,

100% acrylic polymer modified cement base coat that has good water resistance

and vapor permeability.

7.	Finish Coat

Functions as the weathering surface.  It is a factory mixed finish supplied by

STUC-O-FLEX in various colors, finishes and textures.

- 1.02	QUALITY ASSURANCE

Optional but Encouraged - “WaterWay Rainscreen & Ventilation Mats” create space between your building and the elements. They also contribute to air circulation and ventilation when properly designed. Water drainage and increased air flow will enhance drying and in turn reduce the potential damage resulting from water penetration. A Polymer core of fused, entangled filaments in varying thicknesses from a nominal ¼ inch to ¾ inch bonded to a moisture resistant filter fabric on the outer surface.

http://www.stucoflex.com/rainscreen_drainage_mats.html

A.	Applicator Requirements

1.	Applicator shall be licensed, insured and competent to accurately install the 			assemblies consistent with construction documents and specifications. Manufacturer 		is not responsible for application.

B.	Approvals

1.	The assembly shall be recognized for the intended use by the applicable 			building codes.

C. 	Design Consideration

1.	 Deflection of the Substrate system shall not exceed l/240.

2.	 Minimum slope shall be 4 : 12 pitch.

3.	 Expansion Joint Requirements:

a. Where building or substrate expansion joints occur.

b. At floor lines in wood frame construction.

c. Where dissimilar substrates occur.

d. Locations where the system abuts alternate building materials.

e. As determined by design professional

4.	Stuc-O-Flex Coating material terminations to windows, doors, air conditioning 			units, electrical boxes, etc. shall provide adequate space for proper waterproof 			transition. Under no circumstances shall Stuc-O-Flex be responsible for integrity 			or design.

5. 	Stuc-O-Flex Coatings shall terminate at a minimum 8” inches above grade.

6. 	Sealant system shall be compatible with Stuc-O-Flex base Coat and adjacent 			building product.  Consult sealant manufacturers for recommendations

7. 	All insulation board not applied to cementitious surfaces shall incorporate a 				code compliant Weather Resistive Barrier and a mechanism for water drainage 			between insulation and substrate (Option: WaterWay Drainage Mat).

Note: All Stuc-O-Flex transitions to adjacent building materials shall be professionally designed and executed to prevent water intrusion behind the coating materials; this is normally achieved by incorporating a nominal ½ wide backer rod & sealant joint. The integrity of this water tight detail must be maintained. Stuc-O-Flex International, Inc. is not responsible for design.

- 1.03	SUBMITTALS

A.	Samples:

1.	The applicator shall, before the project commences, provide the owner or the 		architect, a sample of suitable size of each color and texture as specified for the 			project for the purpose of obtaining approvals.

2.	Each sample shall be prepared using the same tools and techniques as required 		for the actual application.

3.	An approved sample shall be available and maintained at the job site.

- 1.04.	PRODUCT DELIVERY, STORAGE AND HANDLING

A.	Deliver all material supplied by the manufacturer in original, unopened packages with 		legible manufacturer’s identification and labels intact.

B.	Store all products supplied by STUC-O-FLEX in a cool dry place, out of direct sunlight, 		protected from weather and other damage.  In addition, the materials shall be stored 		in tightly sealed containers at a temperature of not less than 40ºF at all times.

- 1.05	JOB CONDITIONS

A.	Weather and Environmental Conditions

1.	Application of Stuc-O-Flex Coatings shall not take place during inclement 			weather unless appropriate protection is employed.

2.	Stuc-O-Base and Stuc-O-Flex Elastomeric Finish shall be protected against 			freezing temperatures, rain, or water splash for a period of at least 48 hours.  The job 		should be tented and a heat source provided if there is a projected drop in the 			temperature below 40ºF during the first 24 hours after application of Base coat or 			Finish coat.

- 1.06	COORDINATION AND SCHEDULING

A.	The work in this section requires close coordination with related sections and trades.

B.	The tops of all walls must immediately be protected to prevent water infiltration 			behind the exterior wall assembly. The cap flashing should be installed immediately 		after the Finish coat has been cured.

C.	Sealant and waterproofing materials shall be installed in a timely manner as to 			prevent water intrusion behind the Stuc-O-Flex coatings.

- 1.07  MAINTENANCE

A. 	Sealant and other components of the structure must be inspected periodically to 			confirm performance as originally installed. Corrections shall be made at once.

- PART 2 - PRODUCTS

- 2.01	MANUFACTURERS

All Stuc-O-Flex Coating products shall be obtained from STUC-O-FLEX INTERNATIONAL, INC., as

manufacturer, or its authorized supplier or distributor.

Contact: 	Stuc-O-Flex International, Inc.

17639 NE 67th Court

Redmond, WA 98052

800-305-1045	info@stucoflex.com	www.stucoflex.com

- 2.02 MATERIALS

A. 	Insulation Board

Option #1:

Expanded Polystyrene (EPS) Board with an average density of 1.0 pcf, a flame spread 		rating of less than 25, a smoke development index of less than 450, and an R-value of 		3.85 per inch at 75 degrees F.  It must conform to ASTM C 578-85 Class A.

Option #2:

Fiberglass faced Polyisocyanurate Insulation Board with an average density of 2.0 pcf, 		a flame spread rating of less than 25, a smoke development index of less than 450, 			and an R-value of 6.3 per inch at 75 degrees F.  It must conform to ASTM C 578-85 			Class A

B.	 Washers / Mechanical Fasteners

Shall be a 2” inch wide polypropylene washer with a recessed-center chamber to 			accept the corrosion resistant fastener as manufactured by Wind-Lock or equal. 			Fasteners shall penetrate structural members a minimum 3/4” inch.

C.	Fiberglass Reinforcing Mesh

Balanced open weave fiberglass reinforcing mesh, treated for compatibility with other 		materials of the system.  The fabric shall not be less than 4.4 oz (± 10%) per square 			yard.

High Impact Resistant System  (Recommended for first floors, for high traffic areas, and 		areas subject to abuse). This assembly consists of an additional layer of Light Armor (15 		oz.) Mesh or Armor (21 oz.) mesh embedded in STUC-O-FLEX PRM or Stuc-O-Base coat. 		The heavier mesh is always installed under the lighter mesh.  In no case should the 			Armor mesh be used without the regular mesh (4.4 oz) over it.

D.	Base coat

PRM (Polymer Reinforced Mortar) Base or Stuc-O-Base is a fiber reinforced,

100% acrylic polymer modified cement base coat that has good water resistance

and vapor permeability.

E.	Finish Coat functions as the weathering surface. It is a factory mixed Finish supplied by

STUC-O-FLEX in various colors, finishes and textures.

F.	Water - shall be clean and potable.

- 2.03	PROPERTIES

The Stuc-O-Flex coatings comply with following test standards:

| TEST | METHOD | RESULT |
| --- | --- | --- |
| ELONGATION % (FINISH) |  | 105 Percent |
| WATER VAPOR TRANSMISSION | ASTM-E96 | 14 GRAINS PER HOUR / SQ. FT. (AVERAGE) |
| SALT SPRAY RESISTANCE | B-117 | 300 HOURS NO DELETERIOUS EFFECTS |
| ACCELERATED WEATHERING | G-23-81 | 2000 HOURS NO DELETERIOUS EFFECTS |
| ABSORPTION FREEZE THAW | 60 CYCLES | NO CRACKING, CHECKING |
| TENSILE BOND | ASTM C-297 | 127.9 PSI |
| WATER PENETRATION TEST | ASTM-E-331 | NO WATER PENETRATION OCCURRED ON SUBSTRATE |
| WATER RESISTANCE TEST | ASTM D-2247 | NO CRACKING, BLISTERING, PEELING OR COMPROMISE |
| MILDEW / FUNGUS RESISTANCE | 810 B | NO MOLD OR MILDEW GROWTH DURING TEST |
| WIND DRIVEN RAIN |  | NO DELAMINATION, NO WATER INTRUSION |
| FIRE TESTING TUNNEL TEST | ASTM E-84 | FLAME SPREAD < 25 SMOKE DEVELOPED < 450 CLASS "A" FIRE RATED |

- PART 3 - EXECUTION

- 3.01	INSPECTION

A.	Prior to proceeding, carefully inspect preparatory and installed work of other trades 		and verify that such work is correct and completed to the point where this installation 		may properly proceed.

B. 	Substrate shall be dry, sound and free of release agents (silicones, oils, etc.), paint and 		other residue or coatings.

D.       The substrate shall have no planar irregularities greater than 1/4” in 8 feet.

C.	Notifications - The General Contractor and the Architect shall be advised of any 			discrepancies. Work shall not proceed until all unsatisfactory conditions are corrected 		and the substrate is acceptable, clean and free of any contaminants, including 			completion of all appropriate flashing and other waterproofing details.

- 3.02	INSTALLATION

A.	Adhesive and Insulation Board

The following adhesives may be used to attach insulation board to cementitious 			substrates:

1.	STUC-O-FLEX PRM (polymer modified mortar) adhesive / base coat

a.	Mix material in a pail with approximately 2 gallons of clean, potable water 				until a buttery consistency is attained.  As in other cementitious mortar 					mixes, retemper the mixture after about 10 minutes from the time the 					adhesive was originally mixed.

2. 	STUC-O-BASE should be mixed 1:1 by weight with fresh, dry Portland Cement 				type I or II.  Product should be allowed to sit for 10 minutes, then remixed use 				immediately

b.	After mixing apply Stuc-O-Base or PRM Adhesive/Base coat to the entire 				back surface of the board using a 3/8” inch notched trowel.

c.	Install insulation board on the substrate and apply equal pressure over the 				entire board surface to ensure uniform contact and solid adhesion.

d.	Butt all joints tightly to ensure a flat, flush and level surface.  Use straight 					edge as necessary to align and check.

e.	For installation details at rooflines, windows and joints with other materials, 				refer to construction documents & details.

f. 	Any irregularity of the insulation surfaces greater than 1/16” must be 					sanded flush.

B.	Mechanical fasteners – Used for application over code compliant secondary moisture 		barrier:

1.	Use the compression disk to secure the insulation board through the 					substrate to the structural framework.

2.	Make sure the correct fastener type is used for the framing and 						substrate type and the recommended installation pattern is followed.

Fastener shall be countersunk 1/16” and covered with one layer of PRM 				(polymer reinforced mortar) Base coat and allowed to dry prior to the 					application of the full PRM Base coat layer.

C.	Base coat and Reinforcing Fabric

1.	Apply STUC-O-FLEX PRM (polymer reinforced mortar) or STUC-O-BASE, Base 				coat - Using a stainless steel trowel, apply a minimum 1/16” thickness of 				PRM to the entire surface of the insulation board.

2.	Install Reinforcing Fabric

a.	Immediately place the reinforcing fabric against the wet Base 						coat and by troweling from the center to the edges, embed 						the fabric into the Base coat.

b.	The reinforcing fabric must be continuous, free of wrinkles and 						be fully embedded in the Base coat.  All corners and overlaps 						shall be at least 2 1/2”.

c.	For construction not detailed with control joints at door, 							window and other openings, additional “butterfly” strips of 9” 						x 12” regular reinforcing mesh will be embedded within

the PRM coat at a 45 degree angle at each corner during 							base coat application.

d.	Allow at least 24 hours drying time.  Additional time may be 						required at low temperatures or with high humidity conditions.

e.	Where shown on plans, the High Impact System is to be 							installed as follows: the Armor Mesh is first embedded into the 						Base coat.  The Base coat is allowed to dry for 24 hours.  Then 						another coat of Base coat is applied over the first application 						to embed the regular reinforcing mesh.

D.	Finish Coat

1.	Thoroughly mix the STUC-O-FLEX factory mixed Finish coat.  Use a high-speed 				mixer and stir until a uniform consistency is obtained.  If necessary, add small 				amounts of clean, potable water (not to exceed 12 oz. per pail) to adjust 				workability.

2.	Use Finish color and texture as it conforms to previously submitted and approved 			sample.

3.	Use clean stainless steel trowels to apply Finish coat directly over the Base coat.

(Some finishes may be spray applied -- please consult STUC-O-FLEX).

4.	Special texture and grain effects are obtained by troweling.  Consistent 				troweling techniques by all mechanics on the job must be used to achieve 				uniformity of appearance.

E. 	Sealants

1. 	Properly installed Sealant system must be incorporated to prevent water 				intrusion behind Stuc-O-Flex Coating materials

- 3.04	JOB SITE CLEAN UP

A.	All excess STUC-O-FLEX wall coating materials shall be removed from the job site by 		the STUC-O-FLEX applicator.

- STUC-O-FLEX

- “THERMAL-FLEX ”

- Coating Materials Application

- APPLICATION INSTRUCTIONS

Prior to any installation work, the following conditions must be met:

1.	Check that the framing/sheathing is structurally sound, dry, and clean.

2.	The framing/sheathing is in accordance with contract documents and specifications.

3.	Check that the moisture content of the sheathing does not exceed 17%.

4.	Check that all roof terminations, mechanical equipment, decks, windows and doors 		are appropriately flashed to protect against water intrusion.

5.	Code compliant “Weather Resistive Barrier” is properly installed to prevent potential

moisture penetration to substrate is mandatory for compliance, when not applied to 		cementitious surfaces.

Note: Flashings, weather resistive barriers, and waterproof transitions from Stuc-O-Flex Finish to adjacent materials along with good construction practice are critical to long-term performance of the exterior wall coatings

If any of the conditions above are not properly met, immediately notify the General Contractor, Architect, or Owner.  Work should not continue until such time that all unsatisfactory conditions are corrected.

- Step One - Applying Casing Bead with Weep Holes to the Substrate

1.	Application of the casing bead with weep holes begins at the base of a vertical 			surface as follows:

A.	Snap a chalk line at the base of the substrate at all horizontal terminations, 				including but not limited to foundations, floor line expansion joints, roof to wall 			interface, top of penetrations windows, doors, mechanical equipment, etc.

B.	Fasten as instructed by manufacturer.

- Step Two - Installing Insulation Boards with Washers / Mechanical Fasteners

Washers / Mechanical Fasteners shall comply with section 2.02 Materials, Paragraph B,

Prior to installation of any insulation board, detail mesh shall be placed around the 			perimeter of the openings by stapling mesh to substrate. This step provides for proper 		encapsulation of insulation board.

Insulation board joints shall not coincide with corners of windows, doors, or other 			penetrations. This will reduce any potential for cracks in these locations.

1.	Fasteners shall be corrosion resistant in an appropriate length to penetrate structural 		members as required by the manufacturer and code.

2. 	Insulation board may be cut by one of the following methods:

A.	Razor knife and straight edge.

B.	Fine toothed handsaw.

C.	Radial arm saw or table saw with a fine-toothed plywood blade.

D.	Hot wire cutting machine.

3.	Insulation board joints and corners should be staggered. Insulation board should also 		be staggered over the substrate joints (Important). No insulation board joints should 		fall on substrate joints both vertical and/or horizontal, (minimum 8” offset).

4.	Insulation board should be held back from edges when not placed in casing bead 		with weep holes to allow for appropriate caulking details

(Check Architectural Details and Construction Documents).

5.	Installation of mechanical fasteners should proceed as next step.  Make sure the 			correct fastener type is used (either wood, metal or concrete fastener depending 			upon substrate and/or framing member) and the recommended installation pattern is 		followed.  Fasteners shall be countersunk 1/16”, covered with a layer of Stuc-O-Base or 		PRM Adhesive/Base coat and allowed to dry.

6.	Fastening schedule shall comply with construction documents.

7.	If insulation boards do not abut tightly and there is a gap in the joint, the joint must be 		filled with a piece of properly adhered EPS board.  Under NO CIRCUMSTANCES are 			joints to be filled with Adhesive/Base coat.

8.	Rasping of EPS insulation board:  All irregular seams in the EPS board are to be rasped 		smooth.  Generally, the whole board and/or area of wall will require rasping or 			sanding. This can be achieved with Stanley Sur-Form rasp or #16 Grit sandpaper 			stapled to a 2” x 4” or other suitable tool.

9.	While rasping, use a 4-foot straight edge to check the uniformity and smoothness of 		the wall.  Rasping and sanding the EPS board is one of the most important steps in the 		application.  Any irregularities in the EPS board will telegraph through to the finish.

10.	All aesthetic joints can now be produced. Route the joint to the predetermined 			depth, apply adhesive, then embed fiberglass mesh.

Note: 	In the case of router grooves the thickness of insulation board remaining 				shall not be less than 3/4"in any area of the wall surface.

11.	Apply Base coat to the lower section of the board with a trowel, pull up the detail 			mesh and embed in the Base coat prior to embedding the full fiberglass mesh.

12.	Reinforcing fabric is to be wrapped around all edges of insulation board where it will 		abut caulks, foundations, doorjambs, window frames, expansion joints and dissimilar 		materials.  Fabric is to be wrapped over the edge and 3 inches up the front of the 			insulation board.

- Step Three - Embedding Fiberglass Mesh

- 1.	Exterior and interior corners

A.	Pre-cut fabric to 12” width or use STUC-O-FLEX supplied 6” rolls of detail mesh.

B.	Apply PRM Adhesive/Base coat 1/16” to 1/8” thick on EPS board at the corner.

C.	The use of STUC-O-FLEX approved mesh corners is strongly recommended to 				achieve a sharp and impact resistant corner.

D.	Embed fabric with a stainless steel trowel.  (The fabric will act as a screen.)

E.	Final thickness of the adhesive mesh fabric layer shall be approximately 1/16”.

F.	Let cure 24 hours before the next stage of installation.

- 2.	Embedding the reinforcing fiberglass mesh

A.	Pre-cut the mesh to workable lengths.

B.	Apply 1/16” to 1/8” of Base coat to the insulation board.

C.	Trowel mesh vertically into the PRM Adhesive/Base coat STARTING IN THE MIDDLE 			OF THE MESH AND EMBEDDING TOWARD THE EDGES.

D.	Fiberglass mesh should be applied vertically and lapped at least 2 1/2” at all 				edges.

E.	Embed reinforcing 9” x 12” butterfly mesh at a 45º angle at all corners of 				openings where construction details do not provide for joints.

F.	Let cure for a minimum of 24 hours before application of the finish.  Weather 				conditions will affect time needed to cure.

Notes:   Before application of the STUC-O-FLEX Finish:

1)	Make sure the Base coat & Fiberglass mesh layer is dry and hard.  Moisture 				content must be 17 percent or less.  Check, using moisture meter.

2)	Remove any irregularities (trowel marks) with a Goldblatt Sand Stone.

3)	In some instances it may be necessary to skim-coat hollows if the EPS 					board was not perfectly flat.

- Step Four - Application of STUC-O-FLEX Finishes

Mixing Instructions for all STUC-O-FLEX Finishes:

Open pail.  Mix thoroughly with Jiffler mixer, taking care to avoid excessive up and 			down motion with drill and blade.  Too much vertical motion will introduce air into the 		Finish and may inhibit proper curing. Small amounts of water may be added 				(maximum 12 oz.) to adjust workability.

Applications of STUC-O-FLEX Finishes shall commence only when adequate labor 			force and equipment is available to maintain a wet edge insuring a systematic 			installation free of cold joints.

1.	STUC-O-FLEX Finishes

A.	STUC-O-FLEX “T” or “Modified” Finish - Consistency of STUC-O-FLEX Finish will be 			similar to creamy stucco. Color is integral and will dry darker on the wall than 				the shade appears in the pail. Apply STUC-O-FLEX Finish using a stainless steel 				trowel to the thickness of the largest aggregate within the product and float 				smooth for a sand finish appearance. Various textures can be accomplished 				with troweling and floating of the STUC-O-FLEX Finish. Maintain a wet edge. 				Finish thickness must be a minimum 1/16” inch.

B.	PUTZ-FLEX Finish - Coarse, wormy type texture. PUTZ-FLEX is applied with a 				stainless steel trowel and pulled tightly to the largest aggregate. Circular 				texturing is achieved with a stainless steel trowel or plastic float. Vertical 				texturing is achieved with up and down motions 12” to 24” using a wood float or 			plastic float.

2.	Normal temperatures (50 to 70 degrees F.) usually will promote a “dry to the touch” 		condition after 2-3 hours.  Curing time, however, is approximately two weeks.

3.	Observe instructions on the label including - Do not apply when temperature is below 		40 degrees F. or will drop below freezing within 24 hours of application. Finish must be 		protected from direct moisture and freezing temperatures until dry (Normally 24 hours). 		No additives may be used.

NOTE:  All Stuc-O-Flex transitions to adjacent building materials shall be professionally designed and executed to prevent water intrusion behind the coating materials; this is normally achieved by incorporating a nominal ½ wide backer rod & sealant joint. The integrity of this water tight detail must be maintained. Stuc-O-Flex International, Inc. is not responsible for design.

Flashing, Sealant, Proper Design and continued maintenance must prevent water intrusion behind any and all Stuc-O-Flex manufactured materials.